EVEREST EXTERIOR PRIMER 
Product Code: - 0510
Product Information

Everest Exterior Primer is based on 100 % pure acrylic emulsion binder specially for exterior plaster which improves adhesion between top coats & wall .It has design in such way that it will imparts properties like abrasion resistance, non chalking, non peeling & non flaking of top coats like Evershine premium exterior emulsion paint . It has special features like easy brushing, quick drying and good sealing properties. This primer is famous for priming water base paint like premium emulsions, distempers & water base special coatings. To achieve excellent hiding of brilliant & English brighter shades only one primer for exterior can be offer through dealer tinting system with wider mood creating shades.
Technical Data
	Sr.No.
	Physical Properties
	Specification /Observations

	1
	Basic composition
	Binder :- 100% pure acrylic polymer

Pigment :-Inorganic high quality pigment& Extenders
Solvent :- Clean municipal water

	2
	Paint Film Properties
	Due to acrylic tough & hard film withstand exterior atmospheric humidity, water alkali & acid resistance in addition with Special type of preservatives for Incan & anti fading & antifungal properties.

	3
	Finish
	Flat ,Smooth with matt finish

	4
	Appearance or Consistency
	Thick & Buttery

	5
	Specific Gravity in kg/lit
	1.40 -1.60

	6
	Supplied Viscosity on DOP @ 30°C sec
	310 -370 Division on Penetrometer.

	7
	Volume Solids
	Approx  60-70 %

	8
	Method of application
	Brush, Roller or Spray

	9
	Area of application
	RCC,Well prepared concrete, asbestos & plasters

	10
	Drying time @ 29±1°C & RH = 65+/-5

Depend on temperature & humidity
	a) Dry to Touch   = 10 min max.
b) Recoat Time = 3 – 4 hrs.

	11
	*Theoretical Covering Capacity on Smooth surface under normal condition
	8  to 10 Sq meter / litre /2 coats

86 to 107 Sq ft/ litre/2 coats

	12
	DFT min. for Coverage in two coats
	75 to 80 Micron

	13
	Thinner recommended
	Clean Municipal water

	14
	Thinning ratio
	Brush or Roller: - 2 part paint & 1 part water by volume.

Conventional Spray: - 3-4 part paint & 1 part water (10%) by volume.

Airless Spray: - 1.5 part paint & 1 part water (10%) by volume.

	15
	Durability (based on surface & application)
	4 Years minimum.

	16
	Shades or Colors
	As per shade card & Color Bazaar fan deck

	17
	Pack Sizes
	20 Lit , 4 Lit &1Lit


Direction for Use

Surface Preparation
for New Plaster: - New surface should be cleaned and free from efflorescence. New plaster surface must be mature at least for the period of 6 month after the drying of lime wash to ensure through drying then remove all the loose particles of lime wash & then applied thinned Everest exterior primer two coats. 
Surface Preparation
for Old Plaster: - Normally all old plasters are painted with lime wash, cement paint or any previous paint hence it must be scraped thoroughly using sand paper or wire brush .During this repair cracks ,leakage & drainage prior to surface preparation. Old surface must be free from effloresance other wise pretreatment should be given & fungus affected area should be separately treated with our Pashupati Antifungal wash.

Applications Procedure & Recommendation for best Performance: - 
For exterior coating recommended primer is Everest exterior primer only & the system of application based on surface should be followed 

	S.No
	Surface Type
	Step-1
	Step-2
	Step-3

	1
	New Surface
	Primer(1 Coat)

Everest Exterior primer 
	Putty not recommended
Use for filling dents or cracks only
	Primer(1 Coat)

Everest Exterior primer 

	2
	Prepainted prepared Surface.
	Primer(1 Coat)

Everest Exterior primer 
	Finish paint (2 Coats)
	


For priming of exterior walls should be painted with our Everest Exterior primer water thinnable then if required applied Wall guard cement base putty to fill the crakes, dents etc as well as make surface very smooth & free from damp, leakage & fungus then applied two coats of Everest Exterior primer for old plaster can be applied using recommended brush or spray viscosity accordingly add water For  Deep ,English or Brilliant shades use tinted primer using the same formula as of desire shade thorough color bazaar tinting machine which will enhance the hiding ,sheen & real beauty of shade. 
Precaution:

· Keep it out of reach of children 

· Stir well & strain before use as well as fallow safety ,heath & environmental information 
· Do not apply when ambient temperature is less than 10 °C otherwise drying of finish paint will delayed.

· Do not use any other companies universal stainers or colorants 

· Do not over thin & not applied on powdery, chalky & damp surfaces.                       

· Do not expose the primed surface unpainted with the finish coats for a period of more than 24 hrs to avoid premature paint failure.

· Avoid use of plaster of Paris & its mixer to fill dents, gaps & cracks.



· Flash Point: Above 300C (860F)
Safety Heath & Environmental Instruction 
· Container must be in a secure, upright position & keep tightly closed.
· Keep away from source of ignition, food, drink, animal feed& children’s.

· Do not breath vapour or spray , Keeps doors & windows open during applications

· Put on air supplied breathing mask for sanding & painting especially for confined space.

· Put on eye glasses for eye protection in case of eye contact rinse immediately with plenty of water & seek medical advice.

· After application use soap & water or cleaner for hands or skins.

· Disposal of paint should be land filing & do not throw in any drain & water channel. 

Everest Colour P Ltd 
NOTE:  The Information is given in good faith but without any warranty.  We reserve that right to change data without prior notice due to continuous R&D.* Covering capacity is the result obtained on well prepared smooth surface hence it may change from surface to surface.
