EVEREST WOOD PRIMER
Product Information

Everest wood primer especially designs for protection of wood surfaces. It is based on resins; pigments combinations so as to give excellent sealing & filling properties hence it give protection from absorption of moisture in side the wood surface. It can easily penetrate the wood surface fibers which provide extra adhesion power for top coats. It forms very tough & flexible film for to protect the internal wood chemical oozing outs. It provides good alkali, moisture& fungus resistance. It can be easily applied by brush or spray and dries very fast hard to form a good adherent coating.
Technical Data
	Sr.No.
	Physical Properties
	Specification /Observations

	1
	Basic composition
	Binder: - Varnish/Long oil modified alkyd resins.

Pigment:-Best quality inorganic pigment.

Solvent :- White Sprit/Mineral Turpentine oil

	2
	Paint Film Properties
	Due to /Varnish/long oil Flexible, tough film with inorganic white pigment form very strong setting & adhesive film has good humidity, water alkali & acid resistance.

	3
	Finish
	Smooth ,matt finish

	4
	Appearance or Consistency
	Free flowing liquid.

	5
	Specific Gravity in kg/lit
	1.20 – 1.50

	6
	Supplied Viscosity on FCB4 @ 30°C sec
	80-110 second.

	7
	Volume Solids
	Approx  60-75 %

	8
	Method of application
	Brush, Roller or Spray

	9
	Area of application
	Well prepared Wood, Metal&Mansory surface.

	10
	Drying time @ 29±1°C & RH = 65+/-5

Depend on temperature & humidity
	a) Surface dry   = 1 hrs. max

b) Tack Free     = 6 hrs. max

c) Hard Dry      = Over night 

	11
	*Theoretical Covering Capacity on Smooth surface under normal condition
	9 to 14 Sq meter / litre /1 coats 

96  to 150 Sq ft/ litre/2 coats

	12
	DFT min. for Coverage in per coats
	20 to 25 Micron maintain ideally.

	13
	Thinner recommended
	Everest G.P. Paint Reducer.

	14
	Thinning ratio
	· For brushing or roller-- One part WS/MTO to 8 Parts of paint by volume if required add extra to achieve brushing or roller viscosity 55 – 60 second.

· For conventional Spraying-- One part WS/MTO to 12 Parts of paint by volume if required add extra to achieve conventional Spraying viscosity 25 – 30 second.



	15
	Durability (based on surface & application)
	 3 Years minimum.

	16
	Shades or Colors
	White & Pink with all tinted color bazaar shades

	17
	Pack Sizes
	20 Lit , 4 Lit ,1Lit & 500 ml.


Direction for Use

Surface Preparation
: - This product is specially for wood surfaces before to apply surface prepare using rough sand abrasive paper no 180  & make it smooth using sand abrasive paper no 320 in second coa t sanding as well as wood sanding machines.     
Surface Preparation
for painted surface: - Painted wood surface must be clean using Everest paint removal. Surface must be rubbed using sand paper until all loose paint dust, rust & loose particles can be removed using paint removal, solvent, sand paper.

Applications Procedure & Recommendation for best Performance: - 
Everest Wood Primer white or pink can be used on wood stepwise systematic application based on surface should be done as follows 

	S.No
	Surface Type
	Step-1
	Step-2

	1
	Wood Surface
	Wood-filler/ sealer
	Primer(2 Coat)

Everest Wood Primer White/Pink

	2
	Repainted Surface
	As on required
	Primer not required 

If required applied as per surface


The Everest Wood Primer white/pink is applied with recommended thinning ratio for brush & spray application before that ensure the surface is free from moisture and loose particles. The first coat should be wet sanded with water –proof emery paper grade 320-400 before the second coat is applied after application of second coat then cut primer using sand paper for painting top coats.

Precaution:

· Keep it out of reach of children 

· Stir well & strain before use as well as fallow safety ,heath & environmental information 
· Do not apply when ambient temperature is less than 10 °C otherwise drying of finish paint will delayed.

· Do not over thin & not applied on powdery, chalky & damp surfaces.                       

· Do not expose the primed surface unpainted with the finish coats for a period of more than 24 hrs to avoid premature paint failure.

· Avoid use of putty & its mixer to fill dents, gaps & cracks.



· Flash Point: Above 300C (860F)
Safety Heath & Environmental Instruction 
· Container must be in a secure, upright position & keep tightly closed.
· Keep away from source of ignition, food, drink, animal feed& children’s.

· Do not breath vapour or spray , Keeps doors & windows open during applications

· Put on air supplied breathing mask for sanding & painting especially for confined space.

· Put on eye glasses for eye protection in case of eye contact rinse immediately with plenty of water & seek medical advice.

· After application use soap & water or cleaner for hands or skins.

· Disposal of paint should be land filing & do not throw in any drain & water channel. 

Everest Colour P Ltd 

NOTE:  The Information is given in good faith but without any warranty.  We reserve that right to change data without prior notice due to continuous R&D.* Covering capacity is the result obtained on well prepared smooth surface hence it may change from surface to surface.

